## Slide 1
Some Applications of Superconductors
From the Short Course Tutorial
Superconducting Electronics
2024 Applied Superconductivity Conference
Salt Lake City, Utah USA
1 September, 2024
Steven M. Anlage
Quantum Materials Center
Physics Department
University of Maryland
College Park, MD 20742-4111 USA
anlage@umd.edu
https://anlage.umd.edu

## Slide 2
III. Applications of RF Superconductivity
Resonators (Coplanar Waveguide for QC, high-Q for SRF accelerators)
Microwave Kinetic Inductance Detectors
Microwave filters
Josephson-based parametric amplifiers

## Slide 3
Resonators
CPW for quantum computing
high-Q for SRF accelerators

## Slide 4
http://www.phys.unsw.edu.au
The Inductor-Capacitor Circuit Resonator
Idealized Lossless Resonator
resonant
frequency

## Slide 5
Resonators
… the building block of superconducting applications …
Cavity Quantum Electrodynamics of Qubits
Superconducting RF Accelerators
Microwave kinetic inductance detectors
Metamaterials (meff < 0 ‘atoms’)
etc.
Pout
co-planar waveguide (CPW)
resonator
Pin
driving
frequency
f0
|S21(f)|2
resonator
transmission
Port 1
Port 2
Transmitted
Power
CPW Field Structure
coaxial
cable
coplanar waveguide
ground plane
center conductor
[CPW RF Currents]
Co-planar waveguide resonator made from YBa2Cu3O7
[Transmission line resonators]

## Slide 6
Quality Factor
Two important quantities characterise a resonator:
The resonance frequency and the quality factor
Where U is the energy stored in the cavity volume and Pc/0 is the energy lost per RF period by the induced surface currents
Frequency
+Df
= Df
Stored Energy U
Some typical Q-values: SRF accelerator cavity Q ~ 1011 3D qubit cavity Q ~ 108
[Q of a shunt-coupled resonator Detail]
-Df

## Slide 7
What Determines the Q of Resonators?
Assumption: Loss mechanisms are independent and add linearly
Power dissipated
in load impedance

## Slide 8
Microwave Losses / 2-Level Systems (TLS) in Dielectrics
M. Hein, APL 80, 1007 (2002)
Effective Loss @ 2.3 GHz (W)
-60 dBm
-20 dBm
TLS in MgO substrates
YBCO film on MgO
YBCO/MgO
T = 5K
Nb/MgO
Energy
Energy
Low Power
High Power
Two-Level
System (TLS)
Classic reference:
photon
[TLS Microscopics]
[Power in dBm]
The increase in loss as temperature
decreases for -60 dBm is due to the
TLS relaxing back to their ground
state
Notes: A student at ASC 2024 asked about the increase in loss at low-T in the -60 dBm case.

## Slide 9
Resonators
CPW for quantum computing
high-Q for SRF accelerators

## Slide 10: Superconducting Radio Frequency (SRF) Cavity
Grassalino, SRF2019
2017
https://www.lhc-closer.es
cross-section of an SRF
microwave cavity (f0 ~ 1-2 GHz)
Main material: Niobium (Nb)
Tc = 9.2 K, operated at ~ 2 K

## Slide 11
A successful and expanding application of RF superconductivity

## Slide 12
Very good tutorial on SRF cavities for particle accelerators by Anne-Marie Valente-Feliciano (Jefferson lab): https://indico.jacow.org/event/64/contributions/2903/attachments/314/1203/IPAC23-Tutorial-SRFCav_AMVF.pdf
Bulk Nb SRF Cavities and Cryomodules

## Slide 13
Some research topics:
Reproducibly prepare many high-Q cavities
Maximize Q(Eacc)
Find higher-Tc materials for SRF cavities
Higher Q0, larger Eacc
Materials modifications of Nb to improve Eacc
Nitrogen/Oxygen-doping
Replace bulk with thin film Nb on Cu
Prevent / remove trapped magnetic flux in cavities
Understand and eliminate residual microwave loss
Eacc

## Slide 14
Superconducting Microwave Filters

## Slide 15
notch
Superconducting Microwave Filter Application
The electromagnetic spectrum is very crowded
Need to recover weak signals from distant users, and exclude interference
Front-end filter and
low-noise amplifier
Before
After
Low-loss band-pass filter to pass only signals inside allocated band
Add low-noise amplifier on cryogenic platform
Band-pass
filter
[Microwave Filter Application]

## Slide 16
Hongwei Yue, et al., Physica C: Superconductivity 557, 1 (2019)
Microwave Filters are a Collection of Coupled Resonators
DyBa2Cu3O7 film
T = 79.4 K
wide upper stopband
The resonators are implemented
in thin superconducting films

## Slide 17
B. A. Willemsen in H. Weinstock and M. Nisenoff, Microwave Superconductivity. (Springer Netherlands, 2012).
notch
High-Tc Superconducting (HTS) Microwave Filters – Description of Application

## Slide 18
Advantages of HTS Microwave Filters
Small size compared 3D normal metal structures with comparable Q
Low insertion loss in the pass-band
High out-of-band rejection, steep cutoff, narrow-bandwidth and highly selective
Integrate with cryogenic low-noise semiconductor amplifier to improve system SNR
Increased range of reception
At one point (early 2000’s) ~104 HTS filters with cryocoolers in operation in the USA
Microwave filter design
Coupled resonators! Higher Q-factors allows for more aggressive designs. Filter design is a high art
Better performance in filter response requires using more resonators
Typically used to define a band-pass or band-reject filter
HTS microwave filters encouraged the development of:
Low-maintenance stand-alone closed-cycle cryocoolers with long MTBF (~ 5 years between maintenance)
HTS Tc ~ 100 K, operated at about 60 K (N.B. most SC applications require Toperating ~ Tc/2)
Low power, compact, efficient cryocoolers
Two-dimensional (thin film) RF circuits – more compact and easier to cool
Low thermal conductivity microwave cables (connecting R/T-cryogenic)
High-Tc Superconducting (HTS) Microwave Filters – Long-Term Impact
Bulk 3D
normal metal
2D superconducting

## Slide 19
Microwave Kinetic Inductance Detectors

## Slide 20
Geometrical
Kinetic
superconducting
wire
J = Js + Jn
Js
Jn
AC Current-carrying superconductor
T
0
n
nn(T)
ns(T)
Tc
J
n = ns(T) + nn(T)
Js = (-2e) ns vs
As T→Tc, ns ↓, vs↑, to maintain Js
Kinetic Inductance
So the kinetic energy of the Cooper pairs must increase!
as T→Tc
can get very large for
low-carrier density metals (e.g. NbN
or NbTiN), especially if the film width
and/or thickness is <<

## Slide 21
Microwave Kinetic Inductance Detectors (MKIDs)
P. K. Day, et al., Nature 425, 817 (2003)
Integrate a superconducting wire into a compact LC resonator
An absorbed photon breaks a Cooper pair, changes the kinetic inductance of the wire, and shifts the resonance
Monitor the frequency shifts of many resonators (pixels) simultaneously
microwave input
microwave output
absorbed photon
breaks Cooper pair,
decreasing and
increasing
Sensitive to THz-PHz photons

## Slide 22
Multiplexing of MKIDs
Each resonator is a different pixel in an array
Superconductivity provides high-Q resonances
J. Zmuidzinas, Ann. Rev. of Condensed Matter Physics 3, 169 (2012)
16x16 array
of lumped LC
resonators
128 pixels
Transmission
Readout single-photon energies and arrival times
in the imaging array
Notes: 16x16 = 256. (a) A 16 16 array of TiN lumped-element microwave kinetic inductance detectors using a spiral inductor and an interdigitated capacitor. The pixels are approximately 0.6 mm in size. (b) The measured resonances for half the array (128 pixels) are very deep and fall into a 270-MHz band centered at 1.6 GHz. (c) The internal quality factors are very high, Qi > 107 , with good uniformity.

## Slide 23
Josephson-Based
Parametric Amplifiers

## Slide 24
Need to locate amplifier near qubits on the MXC (20 mK) plate –
small cooling power, hence low dissipation required
Amplifier must also have minimal back-action on the qubits
Problem: Recover very small microwave signals from a cryogenic resonator
Amplify the signal (the first of several stages)
Add a minimal amount of noise to the signal
Solution: Use Parametric Amplification to recover the small signal
Dilution
Refrigerator
What is Parametric Amplification?
Josephson-Based Parametric Amplifiers
J. Aumentado, IEEE Microw Mag 21, 45 (2020)

## Slide 25
Parametric Amplification – The Basic Idea
J. Aumentado, IEEE Microw Mag 21, 45 (2020)
Pump energy into the ideal LC-resonant
circuit by modulating the inductance at
twice the resonant frequency, while
utilizing the correct phase.
(called degenerate parametric amplification)
Parametric pump at frequency
Signal to be amplified at frequency

## Slide 26
Gain
1-port
parametric
amplifier
= resonant frequency
of LC circuit
+
Degenerate PA:
Josephson-Based Parametric Amplification
Noise: In the limit the added noise
can approach the standard quantum limit:
J. Aumentado, IEEE Microw Mag 21, 45 (2020)

## Slide 27
Josephson Travelling-Wave Parametric Amplification (J-TWPA)
Signal and Pump tones co-propagate
in the JJ transmission line
One operational mode: “4-wave mixing”
+
C. Macklin, et al., Science 350, 307 (2015)
J. Aumentado, IEEE Microw Mag 21, 45 (2020)

## Slide 28
Advantages:
Operates well at mK temperatures
Virtually no thermal noise is added to the signal
J-TWPA has large bandwidth, slightly noisier
Bandwidth at gain
For example, , results in
Power handling limited by JJ critical current. Typically, setting the limit for practical
input signal powers to lower than –110 dBm (J-reflection PA) or -100 dBm (J-TWPA)
Josephson-Based Parametric Amplification
Challenges:
Limited bandwidth for Josephson reflection PA

## Slide 29
anlage@umd.edu
https://anlage.umd.edu
Some Additional Resources
Steven M. Anlage, “Microwave Superconductivity,” IEEE J. of Microwaves 1, 389-402 (2021). pdf
Introduction to Superconductivity graduate course: https://www.physics.umd.edu/courses/Phys798C/AnlageSpring24/Supp.htm
Numerous sections and chapters in 100 Years of Superconductivity, edited by Horst Rogalla and Peter H. Kes (CRC Press, Boca Raton, FL, 2011).

## Slide 30
Please Ask Questions!

## Slide 31
Supplementary Material Referenced from the above slides

## Slide 32
What are the Limits of Superconductivity?
Phase Diagram
Superconducting
State
Normal
State
Ginzburg-Landau
free energy density
Applied Magnetic Field
Currents
Temperature
Dependence
Tc
m0Hc2
Jc
[Return]

## Slide 33
Transmission Line
Unit Cell
Transmission Line Resonators
Transmission Line Model
Transmission Line Resonator Model
Ccoupling
Ccoupling
[Return]

## Slide 34
SNSPD Photon Detection Principle
Utilize a thin and narrow superconducting wire with high kinetic inductance
An absorbed photon creates a hotspot that spans the wire (ps time scale), turning it into a high-impedance load
The bias current is shunted into an amplifier for detection, the wire cools down and resets
J. A. Lau, et al., Chem Soc Rev 52, 921 (2023)
SNSPD = Superconducting nanowire single-photon detectors

## Slide 35
Microwave Power: dBm vs. Watts. Watts the difference?
dBm means a power relative to W on the decibel scale
is
is
is
Power equivalent to 1 photon/s at 1 GHz is , which is -272 dBm
[Return]

## Slide 36
6 W heat lift at 77 K
100 W power input
Weight: 3.4 kg
MTBF: 579,000 hours
R. W. Simon, et al., Proc. IEEE 92, 1585 (2004)

## Slide 37
A. J. Przybysz, Ph.D. Thesis, UMD (2010)
Grounding the leads prevents
electro-static discharge in to
the device
Isolating the Qubit from External Radiation
Cu patch box helps to thermalize the leads
Low-Pass LC-filter (fc = 10 MHz)
Cu Powder Filter
(strong suppression of microwaves)
The experiments take place in a shielded room
with filtered AC lines and electrical feedthroughs

## Slide 38
Cryogenic Microwave Calibration
J.-H. Yeh, RSI 84, 034706 (2013); L. Ranzani, RSI 84, 034704 (2013)

## Slide 39
Chi Zhang, et al., Superconductivity 2, 100012 (2022)
Microwave Filters are a Collection of Coupled Resonators
S. M. I. Tsuzuki, et al., IEEE Trans. Microw Theory 50, 2924 (2002)

## Slide 40
https://www.nii.ac.jp/qis/firstquantum/e/forStudents/lecture/pdf/noise/chapter11.pdf
Parametric Amplification on a Swing

## Slide 41
Superconducting Quantum Interference Devices (SQUIDs)
The DC SQUID
A Sensitive Magnetic Flux-to-Voltage Transducer
Flux
Ic
Ic
Bias
Current
2Ic
One can measure small fields (e.g. 5 aT) with low noise (e.g. 3 fT/Hz1/2)
Used extensively for
Magnetometry (m vs. H)
Magnetoencephalography (MEG)
Magnetic microscopy
Low-field magnetic resonance imaging
Wikipedia.org
[Return]

## Slide 42
Superconducting Quantum Interference Devices (SQUIDs)
The RF SQUID
A High-Frequency Magnetic Flux-to-Voltage Transducer
R. Rifkin, J. Appl. Phys. (1976)
Not as sensitive as DC SQUIDs
Less susceptible to noise at 77 K with HTS junctions
Basis for many qubit and meta-atom designs
RF SQUID
Tank
Circuit
[Return]

## Slide 43
Microwave Losses Due to Magnetic Flux Motion
Single-vortex response to AC current (Gittleman-Rosenblum model)
Equation of motion for vortex
in a rigid lattice (vortex-vortex force is constant)
Effective mass of vortex
Vortex viscosity ~ sn
Ignore vortex inertia
vortex
Pinning
potential
Frequency f / f0
Dissipated Power P / P0
Pinning frequency 0
Gittleman, PRL (1966)

## Slide 44
where
amplitude for pair
to be missing
probability amplitude for pair
to be present
Cooper pair
creation operator
BCS Theory of Superconductivity
density of states
BCS ground state
wavefunction
Introduction to Superconductivity graduate course: https://www.physics.umd.edu/courses/Phys798C/AnlageSpring24/Supp.htm
[Return]

## Slide 45
The energy scale for binding a pair of electrons is a typical superconductor (meV scale) is much smaller than many solid state interactions and Debye temperature
To find a Hamiltonian for superconductivity, BCS discarded larger interactions terms that were not essential and kept a simple pairing interaction to get a simplified Hamiltonian:
The ground state of the Hamiltonian has the form
where
The uk’s and vk’s are such that is minimized. With simplifying assumptions one finds:
kinetic energy of electron w.r.t. fermi energy m
attractive interaction between electrons with opposite spin and momentum (spin singlet)
[Return]

## Slide 46
pairing symmetry
“Unconventional”
pairing symmetry
“Conventional”
Fermi
surface
SC gap
Superconducting Pairing Symmetries
[Return]

## Slide 47
Abrikosov
Vortex Lattice
Superconductors in a Magnetic Field
The Vortex State
T
H
Hc1(0)
Tc
Meissner State
Hc2(0)
B = 0, R = 0
B  0, R  0
Normal
State
Type II SC
vortex
Lorentz
Force
Moving vortices
create a longitudinal voltage
V>0
I
Vortices also experience
a viscous drag force:

## Slide 48
Bitter Decoration Pb- 4 at % In rod, 1.1 K, 195 G,
Essmann et al. Phys. Lett. 24A, 526 (1967)
Magnetic flux vortices in Type II superconductors
each spot is one end of a vortex tube with
one flux quantum
of magnetic flux
SC
B
Scanning Tunnel Microscopy NbSe2, 1 T, 1.8 K, H. F. Hess et al., PRL 62, 214 (1989)
circulating current around tube of radius l... creates B
center of vortex has superconductivity “suppressed” on scale of coherence length
Type II superconductor has
Courtesy of
Fred Wellstood

## Slide 49
Rapid Single Flux Quantum Logic
superconducting “classical” digital computing
When (Input + Ibias) exceeds JJ critical current Ic, JJ “flips”, producing an SFQ pulse.
Area of the pulse is F0=2.067 mV-ps
Pulse width shrinks as JC increases
SFQ logic is based on counting single flux quanta
SFQ pulses propagate along impedance-matched passive transmission line (PTL) at the speed of light in the line (~ c/3).
Multiple pulses can propagate in PTL simultaneously in both directions.
Circuits can operate at 100’s of GHz
Input
~1mV
~2ps
Ibias
JJ
Courtesy Arnold Silver
[Return]

## Slide 50
Resonators (continued)
T = 79 K
P = - 10 dBm
f = 5.285 GHz
YBCO/LaAlO3
CPW Resonator
Excited in Fundamental Mode
Imaged by Laser Scanning Microscopy*
Wstrip = 500 mm
1 x 8 mm scan
*A. P. Zhuravel, et al., J. Appl. Phys. 108, 033920 (2010)
G. Ciovati, et al., Rev. Sci. Instrum. 83, 034704 (2012)
[Trans. Line Resonator Detail]
[Return]

## Slide 51
What are the two-level systems microscopically?
J. Lisenfeld, et al., Nat Commun 6, 6182 (2015)
C. Müller et al., Rep. Prog. Phys. 82 124501 (2019)
Two-Level System Energies
[Return]

## Slide 52
Fluxoid Quantization
Superconductor is described by a single
Macroscopic Quantum Wavefunction
Consequences:
Magnetic flux is quantized in units of F0 = h/2e (= 2.07 x 10-15 Tm2)
R = 0 allows persistent currents
Current I flows to maintain F = n F0 in loop
n = integer, h = Planck’s const., 2e = Cooper pair charge
Flux F
I
superconductor
Flux F
Circuit C
Surface S
B
Fluxoid
Quantization
n = 0, ±1, ±2, …
[Return]

## Slide 53
Measuring the Q of a Shunt-Coupled Resonator
Ch. Kaiser, Sup Sci Tech 23, 075008 (2010)
[Return]

## Slide 54
High-Tc Superconducting (HTS) Microwave Filters – Description of Application
Its purpose is to minimize the degradation of signal-to-noise ratio (SNR) that occurs in the base station receiver as a natural consequence of detecting and extracting the information content of the desired signals.
The cryogenic front-end accomplishes this by performing two circuit functions extremely well:
1) efficiently and effectively rejecting out-of-band interference, and
2) amplifying in-band signals with extremely low added noise and high linearity.
R. W. Simon, et al., Proc. IEEE 92, 1585 (2004)
[Return]